Failure Analysis of Functional Failures in a Designed for FA SRAM

Gil A. Garteiz, Tower Semiconductor LTD. Migdal Ha’emek Israel

Naturally, devices that are designed for failure analysis are much easier to analyze and have a higher FA success rate than devices that aren’t. This extended abstract presents 3 root cause analyses on an SRAM that was designed for FA. The SRAM is an engineering vehicle for a 0.18um CMOS process.

The SRAM discussed in this paper has common design for FA features such as micro pads on all bit lines, word lines and many logic signals. It also has 3 different power supplies and is divided into 32 blocks of memory whose standby current can be measured individually. But perhaps the most useful design for FA feature is an analogue mode in which the bit line pairs can be accessed through the data lines without the involvement of the sense amps, I/O drivers, or pre driver circuits. By performing a static setup including a specific address, individual memory cells can be accessed and characterized.

There are 4 basic tests used to characterize a cell. They are used to evaluate the inverter N and P Channel transistor operation. A voltage sweep is performed on bit line while holding the bit line bar signal either high or low. Then the signals are reversed and the other half of the cell is evaluated. A schematic of the test and I/V traces are shown in figures 1 and 2.

Another test checks the cell for an internal short between inverter outputs. This is done by sweeping BL and BL bar signals simultaneously with opposite polarities (array VDD=0). Figure 3 shows an I/V trace in this condition for a good cell.

The major challenge with analyzing single bit failures isn’t localization; the cell’s precise address is already known. Rather, it is selecting the physical analysis method that will have the highest chance for success. Cells with open or high resistance contacts can simply be cross-sectioned. Cells with short circuits should be approached with a little more care. Without knowing what is shorted inside the cell, they could be sectioned in the wrong direction or a small defect might be over looked. Sometimes a combination of delayering and FIB is recommended.

Analogue mode cell characterization combined with knowledge of the SRAM’s layout can reveal not only why a cell failed, but also exactly where it failed. Figure 4 illustrates this with a single bit failure.

The cell characterized in figure 4, showed no current flow through one of the P-Channel transistors while the N-Channel transistor was fine. This indicates there must be a problem with either the VDD or P-channel inverter output contact. In this SRAM, vertically adjacent cells share a VDD contact. Because only a single bit failed, the VDD contact must be good. Therefore, the P-Channel inverter output contact is open. FIB x-section showed (figure 5), as expected, an open contact. Note that if a high resistance issue was expected, a TEM specimen could have been prepared because of the precise knowledge of this failure.

Cells with short circuits are more difficult to analyze physically because it isn’t always possible to know precisely where the defect causing the short is. It is possible however, to measure the short resistance. This can shed light of the nature of the short. Figure 6 shows I/V traces of shorted cell. After layer removal of the shorted cell, SEM inspection showed “bridged contacts” (figure 7). We wanted to perform TEM on a similar cell and used the short resistance as criteria for selection. This helped to better understand the failure mechanism (figure 8).

Analogue mode operation does not only have to be used exclusively on single bit failures. It can be used to aid localization techniques such as photoemission or TIVA. In SRAM devices with bit line failures, analogue mode can provide a direct connection to bit line to ground shorts, and even bit line to neighboring bit line shorts. Figure 9 shows a bit line to GND short. The added signal obtained by working directly with shorts inside the SRAM array should improve localization signals.

Analogue mode has also been used to help localize failures of entire outputs within blocks (group 16 bit lines in an output). Characterization of the failing output showed a leakage to ground. Photoemission microscopy shown in figure 10 pinpointed the failure site, and subsequent FIB x-section (figure 11) showed a metal defect.

The value of analogue mode operation for FA has clearly been shown for several common functional failures in SRAM. If accepted, my submission to ISTFA would have a few more analyses, defects, and explanations.

Figure 1.	Schematic showing the setup for evaluating transistors in one of the cell’s inverters.

Figure 2.	Resulting I/V traces of N-Channel (purple) and P-Channel (blue) inverter transistors.

Figure 3.	Resulting I/V trace of a good cell checked for an internal short circuit. No current through the origin is observed.

Figure 4. 	I/V traces of an inverter in a bad cell. No P-Channel current flow is

detected.

Figure 5.  Open contact discovered in failing single bit cell.

Figure 6. I/V traces from a cell with an internal short about 10Kohm between inverter outputs.

Figure 7. A contact bridge is found after layer removal

Figure 8. Low mag TEM image of the contact bridge. Note the image is rotated.

Figure 9. I/V trace of a BL to GND short found on a failing bit line.

Figure 10. Emission from the defect location causing 16 bit lines to fail.

Figure 11. FIB x-section from the emission site in figure 10 showing two shorted metal lines.

# Text boxes

M1

M1

Array VDD = 1.8V

BL bar

1/0

WL on by analogue mode

BL

V sweeps