[Standard page, 500 words] r Series in Materials Science 319, https://doi.org/10.1007/978-981-16-5497-8_1 1 nanomaterials and nanotechnology have started to play an increasing role in promoting the progress of Sci-Tech and economic development. The subsequent discovery of carbon nanotubes (CNTs) in 1991 has attracted continuous and extensive attentions in various fields due to unique atomic structures and structural-depended properties. In particular, single-walled CNTs (SWCNTs) have been demonstrated to fabricate higher performance electronic, optoelectronic, photovoltaic, and sensing nanodevices. The first preparation of graphene in 2004 made it have a great potential to the application in photonics, optoelectronics, transparency electronics, and so on. Together with new carbon allotropes (atomic carbon chains and graphdiyne): the properties and application fields of carbon materials will be further expanded in 21st century. Therefore, the development of these carbon allotropes is promoting mankind into a new era of carbon, [3] in which carbon nanomaterials and nanodevices will be widely used in the next-generation information processing technology, and the performance of carbon-based integrated circuits will be much higher than those of silicon [4, 5]. Actually, the unique properties and abundant types of carbon materials are essentially determined by the nature of electronic structure and the hybridization states of carbon atoms. A carbon atom contains six electrons with the following electron configuration: (1s)2 (2s)2 (2p)2 . The small energy difference between the 2sand the 2p- orbital electrons makes it easily to excite one electron from the 2s state into the 2p-state, resulting in the formation of spn -hybrid orbital (n = 1, 2, 3) by mixing 2s- and the 2p- orbitals. Consequently, carbon atoms can form more valence bond configurations, various atomic arrangement structures and allotropes, while none of the other elements have this ability. In the spn -hybridization, the (n + 1) electrons in hybrid orbitals form a r-bond, while additional unhybridized [4 − (n + 1)] electrons in 2p- orbitals form a p-bond. Obviously, there are only r-orbital electrons in sp3 -hybridized materials (eg. Diamond): which involve the C–C bonding with a large binding energy and distribute in the direction of C–C binding axis. However, for most carbon materials, p-orbital electrons are also involved and distribute perpendicular to the C–C bonding axis, which can move freely in the nonlocal conjugated system formed inside and on the surface of the crystal and molecules, forming a p-orbital electron cloud in sp2 - and sp- hybridized materials. More importantly, r-orbital electrons are sensitive to the change of physical and chemical environments, making carbon materials exhibit a variety of unique properties. The unique electron configuration and multiple chemical bonding possibilities enable the formation of a large number of carbon allotropes, such as diamond, graphite, and amorphous carbon. The Nobel Prize-winning discovery of fullerenes (C60) in 1985 has inspired remarkably research interest in carbon allotropes and carbon nanomaterials, and the subsequent discoveries of SWCNTs and graphene open up exciting new possibilities for carbon era. Nowadays, different carbon allotropes have been discovered and synthesized, and their electron orbital hybridizations can be summarized in Table 1.1. Except for diamond, unique

Below is using the “headings” to write down the whole book.

We can generate the contents automatically from the headings.

Chapter 1.	第1集，office 2013 标题如何设置多级列表	2

1.1.1.	word 2013 标题如何设置多级列表	2

1.1.2.	word 2013 标题如何设置多级列表	3

1.1.3.	word 2013 标题如何设置多级列表	3

Chapter 2.	第2集，word 2013 标题如何设置多级列表	5

2.1.	word 2013 标题如何设置多级列表	5

2.1.1.	word 2013 标题如何设置多级列表	5

2.1.2.	word 2013 标题如何设置多级列表	5

Chapter 3.	第3集，word 2013 标题如何设置多级列表	6

3.1.	word 2013 标题如何设置多级列表	6

Below is the chapters to write the book by using the “headings” to as the outlines.

Heading1，office 2013 标题如何设置多级列表

Heading2

Heading3 word 2013 标题如何设置多级列表

https://www.baidu.com/s?ie=UTF-8&wd=office+2013+%E6%A0%87%E9%A2%98%E5%A6%82%E4%BD%95%E8%AE%BE%E7%BD%AE%E5%A4%9A%E7%BA%A7%E5%88%97%E8%A1%A8&bn=centbrowser

word 2013 标题如何设置多级列表

aa

word 2013 标题如何设置多级列表

bb

第2级heading2 ，word 2013 标题如何设置多级列表

word 2013 标题如何设置多级列表

https://jingyan.baidu.com/article/1876c852468dd8890b1376a9.html

word 2013 标题如何设置多级列表

word 2013 标题如何设置多级列表

word 2013 标题如何设置多级列表

word 2013 标题如何设置多级列表